## Slide 1: Lecture 13 (Low dimensional) Quantum Confined Structures (quantum wells, 2D semiconductors & quantum dots)
Read: FS6
Atomically thin MoS 2: a new direct-gap semiconductor KF Mak, C Lee, J Hone, J Shan, TF Heinz Physical Review Letters 105 (13), 136805

## Slide 2
Angled incidence
Grating on surface
(even normal incidence)

## Slide 3: Quantum Cascade Laser
60 nm
520 meV
3
2
active
region
injector (n-doped)
injector (n-doped)
e
active
region
J. Faist, F. Capasso, et al. Science 264, 553 (1994)
From IR/MIR/FIT to THz!

## Slide 4: Fabrication: MBE or MOCVD TEM / SEM image
55 nm
0.9 nm thick
well and barrier

## Slide 5
2D semiconductor material (eg. Transition Metal DiChalcogenides)
See reviews: Q.H. Wang et al. Electronics and optoelectronics of two-dimensional transition metal dichalcogenides, Nature Nanotechnology 7, 699–712 (2012); X Xu, W Yao, D Xiao, TF Heinz, Spin and pseudospins in layered transition metal dichalcogenides, Nature Physics 10 (5), 343-350 (2014)
Nature Nanotechnology
Volume:
  7,
Pages:
  699–712
Year published:
  (2012)
Nature Nanotechnology
Volume:
  7,
Pages:
  699–712
Year published:
  (2012)
Nature Nanotechnology
Volume:
  7,
Pages:
  699–712
Year published:
  (2012)
Bulk:
1.3eV
indirect
1L:
1.9eV
direct

## Slide 6
Crystal
structure
(taken from calculated bandstructure in
W. Huang et al. Phys.Chem.Chem.Phys’14)
1L
1L: Breaks
InvSymm
(bulk)

## Slide 7
(taken from calculated bandstructure in W. Huang et al. Phys.Chem.Chem.Phys’14)
[see also: Splendiani, A. et al, NanoLetter, 2010; Wickramaratne et al.JAP’14]

## Slide 11
Bulk gap: 1.85eV (CdSe) 1.5eV (CdTe)

## Slide 12
“inverted lens” shape
Strained
induced
“Stranski-Krastanow” growth regime

## Slide 14: Some general trend when lowing to lower Dimension
Stronger emission (Stronger e-h wavefunction overlap)
Stronger exciton binding
Higher temperature operation
Size dependence (quantum confinement), smaller size blue shift of transition
More tunable
Lower degeneracy (lower symmetry) [different mass no longer degenerate]

## Slide 15
They do evolve b/t each other with size

## Slide 16: Applications in Quantum Photonics ---- single photon sources/quantum emitter (quantum dot)
“The fastest triggered single-photon sources to date have been demonstrated using epitaxially grown semiconductor quantum dots (QDs), which can be conveniently integrated with optical microcavities. Recent advances in
QD technology, including demonstrations of high temperature and telecommunications wavelength single-photon emission, have made QD single-photon sources more practical.”
Quantum opto electronic devices
(electrical & optical control & readout)
(InAs)

## Slide 18: photodetectors
Quantum well
Quantum wire (nanowire)
Quantum dot
(almost) anything…

## Slide 19: QWIP (quantum well infrared photodetector)
Bound to continuum
Bound to bound (tunneling)
See also (discuss later):
Graphene/2D materials based photodetectors
(new/different mechanisms…)

## Slide 20
(Si)
ZnO
Many semiconductors…
later also to discuss superconductor NW single-photon detectors (different mechanism)