## Slide 1: Lecture 18 Luminescence Centers
Read: FS9
(Al2O3 “sapphire” with different colors)

## Slide 2: Topics
Basic physics:
  Vibronic aborption & emission
  Crystal field effect
Luminescence Centers
  Color centers
    F-centers etc. in alkali halides
    NV center in diamond
  “Paramagnetic impurities” in ionic crystals
    Rare earth ion (eg Nd3+ in YAG)
    Transition metal ion (eg. Ti3+ in Al2O3)
Applications
  Solid state based light generation (laser, LED/phosphor etc.)
  Quantum information & photonics
(pump)
ruby

## Slide 3
Slide credit: T. Justel

## Slide 4: Atom-like (emitter) in a solid (host lattice)
defects
Dopants (“ion”)
Conduction
Band (host)
Valence
Band (host)

## Slide 5: Luminescence systems/materials
Slide credit: T. Justel
Defects or dopants

## Slide 6: (simplified) general picture
Conduction
Band (host)
Valence
Band (host)
g
e
(defect/donor levels)
Host lattice is an insulator (semiconductor)
  Electronic band structure
  Phonon (bands)
Luminescence center (defect/dopant)
  Atom-like “emitter”
  “in-gap” two/few-level systems
  Electronic levels/states coupled to host lattice
  vibration (continuum/phonon bands)
Vibronic absorption & emission
(basic idea similar to molecules) but:
Localized atom-like electronic (optical) excitation
+ extended phonons (vibration) in host lattice
(contrast to local electronic + local & discrete vibration in molecule)

## Slide 7: Vibronic absorption and emission
Localized atom-like electronic (optical) excitation
+ extended phonons (vibration) in host lattice
(contrast to local electronic + local vibration in molecule)
g
e
(vibronic bands)
Stokes shift
‘zero phonon line’
Meaning of
“configuration coordinate”
E-vib/phonon
couplingline broadening

## Slide 8: Color Center/Defect Center: F-centers
(in alkali halides)
http://education.mrsec.wisc.edu/background/F_center/index.htm
Produced by:
excess cation..
irradiation..
~1/a2 dependence

## Slide 9
~1/a2 dependence
“Electron in box”

## Slide 10
Absorption and Emission Spectrum Bands of F Center in KCl
Strong e-vibron/phonon coupling
May be used for widely tunable laser
Also more complicated color centers eg. “F2+ center” …

## Slide 11: Nitrogen-Vacancy (NV) centers in diamond
NV0, NV- (common),…
ISC
Excited state
(3E)
Ground state (3A)
1A
m = +1
m = –1
m = 0
m = +1
m = –1
m = 0
2.9 GHz
S=1 (triplet)
S=0
Crystal field splitting
1.4 GHz
1.95 eV
(ZPL)
NV
SiV

## Slide 12: Optical Pumping & Readout
ISC
1A
m = +1
m = –1
m = 0
m = +1
m = –1
m = 0
ESR
Initialization: m = 0 state
Readout (PL): population of m = 0
Excited state
(3E)
Ground state (3A)

## Slide 13
10 µm
Jelezko
How to produce NVs
Natural
Irradiation
implantation
Interesting for
Quantum info/photonics/spintronics
Can address/control individual NV
(optically)  single photon source
2-level system in ground state
(qubit)
ESR (microwave)
to manipulate spin (qubit)
Long spin coherence time
(>ms @RT)

## Slide 14: Sensitive Magnetometer
http://www.diadems.eu/page/en/nv-center-properties.php

## Slide 16: “Paramagnetic Impurities” (Dopants/Ions) in Ionic Crystal
Transition
metal
Rare-earth
(smaller radius,
weaker coupling)
(larger radius,
stronger coupling)
crystal field effect vs. (screened) SOC~Z2

## Slide 17: Rare-earth ions: 4f electrons
Common 3+ ions:
Ce3+
Pr3+
Nd3+
Pm3+
Sm3+
Eu3+
Gd3+
Tb3+
Dy3+
Ho3+
Er3+
Tm3+
Yb3+
(also have divalent forms)

## Slide 18
2S+1LJ (ground state term --- Hund’s rule)

## Slide 19: Nd3+ ion
S=3/2, L=6, J=9/2
(crystal field
splt)
Relative weak effect by host crystal
Commonly put in Y3Al3O15 (“YAG”) etc.

## Slide 20: Nd3:YAG laser
Freq. double:
532nm
Pumped at ~800nm (diode laser or lamp)

## Slide 21: Er3+ doped fiber

## Slide 22: Transition-metal ions: 3d electrons
Ti3+: Al2O3
(Ti:Sapphire)
Widely tunable
Laser!
Time-linewidth
relation:
ft~1
Can generate
ultrafast (fs) pulsed
laser!

## Slide 23: Phosphors and Solid State Lighting