## Slide 1: Lecture 8 Interband Transitions Excitons
Read: FS 4

## Slide 2: Textbook 1: M. Fox “Optical Properties of Solids” (2nd ed, Oxford)
Online pdf (1st ed) seems to be available (google)
“FS”
We’ll cover a good portion of FS
+ selected modern topics

## Slide 4
“-” for emission;
“+” for absorption

## Slide 5: Effect of Electric Field on Interband Transition: Franz-Keldysh Effect & oscillations
Figure 9: (a) Schematic depiction of the Franz-Keldysh effect. The solutions of Schrödinger’s equation with additional electric potential are Airy functions, which decay exponentially into the forbidden gap region. This fact results in increased absorption of photons with less energy than the gap energy (see also b). The absorption change of photons with higher energy than the gap energy shows an oscillatory behavior due to interferences of airy functions in the conduction band.
http://cms.uni-konstanz.de/en/physik/leitenstorfer/research/multi-terahertz-physics-and-technology/
See also: P. Y. Yu, and M. Cardona "Fundamentals of Semiconductors"
Allows absorption below Eg
FS Ex. 3.14

## Slide 6
Ways to apply E-field/voltage: capacitor (gate, may need high V for large E), pn junction, ..
(Klinshirn-Ch16)
“photovoltage excitation
spectroscopy”
Applications of FK effect:
Electro-optical modulation
(n, k, reflectance…)

## Slide 7: P/N and P/i/N junctions: a practical way to apply/tune (large) E-field in (bulk) semiconductors
S. Yoshida et al. “Nanoscale probing of transient carrier dynamics modulated in a GaAs–PIN junction by laser-combined scanning tunneling microscopy”, Nanoscale, 2012,4, 757-761
Reverse bias
forward bias
Vpn>0
Vpn<0
Vbi
Have more well-defined
“i” region and E-field:
E=(Vbi-V)/Li
FS Appendix E

## Slide 8: Excitons: “AMO physics in Solid State Physics”
FS Chap 4
+
-
(small gap)
(large gap material)
Excitons are (bosonic) atom like objects!
Caveat/challenge: usually short life-time
& in a “complex” environment
An exciting frontier in quantum photonics
Coulomb attraction b/t e-h:
 Can increase opt. transition
More like excitation inside atom/mol
Important for exciton:
Binding energy; size;
life time  line width;
(kT…)

## Slide 9: Positronium (“exciton of vacuum”)
Lifetime ~0.1ns (para)-~0.1 s (ortho)
Notes: No such para/ortho for exciton?
<number>

## Slide 10: Review: Hydrogen Atom (Z=1)
Bohr model
Schrodinger equation
“Hydrogenic” atom /ion
Dopant in semiconductor..
(free) exciton (positronium)

## Slide 11
En=-RX/n2
rn=n2aX
[relaxed by factor of few:
LO phonons]
Ex. Estimate for GaAs
Decay channel…

## Slide 12: A few general conditions for (free) excitons
(direct gap)
Exciton @
k=0 only!
(band edge)
match vg
need insulating (undoped) samples
Carriers would screen the
Coulomb interaction & reduce binding
kT is important… (carriers, phonons)

## Slide 13
Direct bandgap good, but not required
(“indirect exciton” in Si & Ge)
e
+h

## Slide 14
(Klingshirn)
See also FS Table 4.1
Larger Eg:  down, (n down),
mass up
[think largest Eg—vacuum!]
Compare
T scale!
1meV~10K
(2.7nm)
(3nm)
(aX~100nm)
No longer
Wannier-Mott
“free” exciton
(aX~13nm)

## Slide 15
Coulomb interaction effects (e-h) even w/o excitons
“H atom” in GaAs!

## Slide 16
E-field effect
Compare External vs “internal” field (or energy)
“AMO” meets electronics!

## Slide 17
An Example of Wannier-Mott Excitons
exciton progression
fits the expression
ν[cm-1] = 17,508 – 800/n2
corresponding to
μ = 0.7 and ∈ = 10
The absorption spectrum of Cu2O
at 77 K, showing the exciton lines
corresponding to several values
of the quantum number n. (From
Baumeister 1961).
Quoted from Figure I.D.28.
Electronic Processes in Organic
Crystals and Polymers by M. Pope
and C.E. Swenberg

## Slide 18: Magnetic Field effect
External: Cyclotron (magnetic) energy
vs
Internal: (excitonic) Rydberg energy RX
Weak B field (diamagnetic perturbation) vs strong B field regime (LL)
Interesting direction:  Explore H-atom physics (AMO) in solid state system?
(E-field effect, B-field effect, spectroscopy, collision/dissociation,
H2 molecules, BEC…)
EB2

## Slide 19
“Mott density”
Excitonic
Gas
Biexciton/molecule
(if dissociate:
e-h plasma)
Liquid/droplet
BEC(?!)
Caution: lifetime
Nature. 443 , 409 (2006).
Exciton density  laser P!
Gen vs recomb.

## Slide 20: Exciton BEC (?)
Candidates:
Cu2O & CuCl (large gap semiconductor)
Coupled GaAs quantum well [Chap FS 6]
  Emerging: Stacked 2D semiconductors (TMDCs)?
Exciton-polariton (exciton+photon) BEC
J. Kasprzak et al. Nature 443, 409 (2006)
[CdTe QWs in microcavity]
See review in T. Byrnes et al. Nature Physics 10, 803–813 (2014)
http://butovgroup.ucsd.edu/condensation.html
Bose-Einstein Condensation of Excitons and Biexcitons, S.A.Moskalenko, D. W. Snoke, Cambridge Univ Press'2000
(May come back this)

## Slide 21
Tightly bound
Small
~Room T
Atom/molecular
nature
Transport:
Hopping through
Lattice?
Strong “polaronic”
(phonon) self-trapping
effect.
Important in conj polymers eg. PDA..
organic LED/laser… biology!

## Slide 22
Reflectivity measurement on different thickness
(distinguish Interference effects)

## Slide 23: Periodic Table of Elements