## Slide 1: Lecture 9 Excitons (cont.) Luminescence (Interband Emission)
Read: FS 4-5

## Slide 2: Textbook 1: M. Fox “Optical Properties of Solids” (2nd ed, Oxford)
Online pdf (1st ed) seems to be available (google)
“FS”
We’ll cover a good portion of FS
+ selected modern topics

## Slide 3: Excitons: “AMO physics in Solid State Physics”
FS Chap 4
+
-
(small gap)
(large gap material)
Excitons are (bosonic) atom like objects!
Caveat/challenge: usually short life-time
& in a “complex” environment
An exciting frontier in quantum photonics
Coulomb attraction b/t e-h:
 Can increase opt. transition
More like excitation inside atom/mol
Important for exciton:
Binding energy; size;
life time  line width;
(kT…)

## Slide 4
“Mott density”
Excitonic
Gas
Biexciton/molecule
(if dissociate:
e-h plasma)
Liquid/droplet
BEC(?!)
Caution: lifetime
Nature. 443 , 409 (2006).
Exciton density  laser P!
Gen vs recomb.

## Slide 5: Exciton BEC (?)
Candidates:
Cu2O & CuCl (large gap semiconductor)
Coupled GaAs quantum well [Chap FS 6]
  Emerging: Stacked 2D semiconductors (TMDCs)?
Exciton-polariton (exciton+photon) BEC
J. Kasprzak et al. Nature 443, 409 (2006)
[CdTe QWs in microcavity]
See review in T. Byrnes et al. Nature Physics 10, 803–813 (2014)
http://butovgroup.ucsd.edu/condensation.html
Bose-Einstein Condensation of Excitons and Biexcitons, S.A.Moskalenko, D. W. Snoke, Cambridge Univ Press'2000
(May come back this)

## Slide 6
Tightly bound
Small
~Room T
Atom/molecular
nature
Transport:
Hopping through
Lattice?
Strong “polaronic”
(phonon) self-trapping
effect.
Important in conj polymers eg. PDA..
organic LED/laser… biology!

## Slide 7
Reflectivity measurement on different thickness
(distinguish Interference effects)

## Slide 9
(<ps)

## Slide 14
Ef>>kT

## Slide 16: Optical orientation
Luminescence polarization
P=(I+I-)/(I++I-) max 25%
=P0/(1+/s)
s :spin relaxation
(mechanisms: SOC such as EY, DP; BAP..)
1/TS=1/+1/s
Hanle effect

## Slide 17
Materials issues:
Bandgap
“Lattice match”
Doping n&p (esp.p)

## Slide 18
Later: new opportunities with Van der Waals (vdW)
“stacked” heterostructure of 2D material semiconductors: no lattice match!

## Slide 19: P-type doping challenge
Esp. Wide gap semiconductor (mh, )  deep acceptable level -> few holes in room T
Critical for p-n junction and optoelectronics (LED, laser…)
P-type GaN breakthrough: annealing
(Nakamura et al.’95  Nobel prize)
Blue & all-color LED Solid state lighting

## Slide 21
Also: scintillators (X/gamma rays, neutrons, any high energy particles), cf. Glenn Knoll book

## Slide 22
Lecture 10 & 11 (Thurs & next Tues) by guest lecturers
  Prof. Tongcang Li, Lec 10 on light source and detectors
  Mr. David Blasing, Lec. 11 on Bloch spheres
HWK 3 posted, due Thurs 2/18

## Slide 23: Periodic Table of Elements